Wide-Temperature Tolerant Cellulose-Based Gels: Design Strategies, Mechanistic Insights, and Emerging Applications​

Abstract

Cellulose-based gels represent a promising class of sustainable materials for emerging applications in soft electronics and biomedical devices that require operational reliability across a wide temperature range. However, their inherent water content sensitivity makes them susceptible to freezing at subzero temperatures and dehydration at elevated temperatures, limiting their practical utility. This review comprehensively summarizes the recent advances in the rational design of wide-temperature tolerant cellulose-based gels. It begins by elucidating the fundamental mechanisms governing water-state regulation and ice crystallization inhibition within polymer networks. Subsequently, this review categorizes and assesses a spectrum of design strategies, encompassing the incorporation of cryoprotectants and organic solvents, the construction of specific network structures, and biomimetic approaches inspired by natural organisms. Special emphasis is placed on the unique role of cellulose’s molecular structure and nano-architecture in achieving enhanced environmental resilience. Furthermore, the review highlights the burgeoning applications of these robust gels in flexible sensors, energy storage devices, and soft robotics under extreme conditions. Finally, we discuss the current challenges and future research directions, aiming to inspire the development of next-generation sustainable gel materials with all-climate performance.

Keywords: Cellulose; Gels; Wide-temperature; Anti-freezing; Water

1. Introduction

The rapid evolution of soft electronics, wearable devices, and intelligent packaging has created an urgent demand for functional materials that can maintain reliability under extreme thermal conditions, ranging from Arctic exploration and high-altitude aviation to deep-sea operation, frozen food logistics and biomedical storage. This operational shift from controlled laboratory environments to real-world scenarios exposes a fundamental limitation of conventional soft materials, particularly ​​hydrogels​​. These applications demand functional materials that exhibit unwavering reliability across a vast thermal spectrum, often spanning from -80 °C to well above 80 °C. Their high water content makes them inherently susceptible to freezing at subzero temperatures, leading to catastrophic loss of elasticity and conductivity, and to dehydration at elevated temperatures, resulting in irreversible structural collapse. This thermal vulnerability restricts their practical application across a spectrum of advanced technologies.

In the quest for sustainable alternatives, research has progressively shifted from synthetic polymers to biomass-based gels. While synthetic hydrogels often face challenges related to biocompatibility, environmental persistence, and reliance on petrochemical resources, biomass gels derived from natural polymers offer inherent advantages of renewability, biodegradability, and often, superior biocompatibility. Among the plethora of natural polymers, ​​cellulose​​ emerges as a structurally ideal and unparalleled platform for engineering wide-temperature tolerance, offering advantages that extend far beyond its well-cited renewability and biodegradability The molecular architecture of cellulose, featuring a linear chain of β(1→4) linked D-glucose units with a ​​dense array of hydroxyl groups​​, provides an unparalleled capacity for forming intensive hydrogen bonds. This innate characteristic is the cornerstone for multi-scale structural design, allowing precise molecular-level interactions with various functional agents, such as ions (e.g., Ca2+, Li+), cryoprotectants (e.g., glycerol, glycols), and organic solvents (e.g., DMSO), that effectively disrupt ice crystal formation and lock water molecules within the network, thereby imparting profound freeze resistance and moisture retention. Furthermore, these hydroxyl groups serve as readily accessible sites for chemical modification and the construction of robust, dynamic supramolecular networks with other polymers (e.g., polyvinyl alcohol, polyacrylamide, lignin, alginate), leading to gels with exceptional mechanical strength and thermal stability that often surpass the performance of synthetic counterparts.

The strategies for achieving wide-temperature tolerance in cellulose-based gels have evolved from simple additive blending to sophisticated multi-scale rational design, primarily governed by several core physicochemical mechanisms. (i) ​​Water state regulation​​. The introduction of ions/salts form strong associations with water molecules, significantly depressing the freezing point through colligative effects and reducing evaporative loss. (ii) ​​Ice crystallization inhibition​​. The use of hydrogen-bond competitors like glycerol or DMSO, which integrate into the water structure, preventing the nucleation and growth of ice crystals even at subzero temperatures. (iii) Construction of organic, ionic liquid (IL) or deep-eutectic solvent (DES) systems​​ that replace water entirely or in part, creating inherently non-freezing gel matrices. (iv) Dynamic network engineering​​. The design of networks incorporating dynamic covalent bonds (e.g., boronic ester bonds, imine bonds) and supramolecular interactions (e.g., hydrogen bonds, metal-ligand coordination) that can dissociate and re-associate, providing remarkable energy dissipation and self-recovery properties under thermal stress. (v) Nano-reinforcement​​ with materials like nano-diatomite, zeolites, MXenes, or clay to enhance mechanical integrity and thermal resilience across temperatures. These strategies collectively manipulate the material’s properties at the molecular, nano-, and micro-scale to defy environmental extremes. Figure 1 summaries the design strategies for cellulose-based gels with wide-temperature tolerance.

Figure 1. The strategies for achieving wide-temperature tolerance in cellulose-based gels.

Despite significant progress, a critical gap exists in the literature, the lack of a comprehensive review that systematically deconstructs the ​​intrinsic relationship between the multi-scale structure of cellulose, the chosen design strategy, the underlying mechanisms, and the resulting macroscopic performance​​ tailored for diverse applications. Current reviews often focus on a single application domain, such as flexible sensors, overlooking the broader, cross-cutting potential of these materials. Although some reviews have talked about the low temperature tolerance of soft gels, they have not reviewed the wide temperature resistance of cellulose-based materials, and lack a summary of the application of soft gels in the field of wide temperature resistance. This review is designed to fill this void by providing a holistic and mechanistic overview of recent advances. We will meticulously analyze the fundamental ​​molecular-level mechanisms​​ of anti-freezing and water retention, linking them directly to the unique chemistry of cellulose. A critical evaluation of advanced ​​design and preparation strategies​​ will be presented, emphasizing the rational selection of components (e.g., ions, solvents, polymers) for targeted performance. Crucially, this review will extensively explore the burgeoning ​​applications of these robust gels​​ across a wide spectrum of fields, demonstrating their versatility not only in ​​flexible electronics and sensors​​ but also in ​​active food packaging​​ for quality preservation, ​​advanced biomedical dressings​​ for cryopreservation or low-temperature therapy, ​​anti-icing coatings​​, and ​​environmental remediation​​ under harsh conditions. Finally, we will critically discuss the persisting challenges, such as balancing long-term stability with biodegradability and scaling up production, and future research directions, aiming to inspire the development of next-generation cellulose-based gels with true all-climate, multi-domain performance.

2. Mechanisms of water retention and freeze-resistance in gel​ materials

​​2.1 Water states and phase behavior in hydrogel networks​​

The fundamental mechanisms for achieving wide-temperature tolerance in hydrogels revolve around the precise manipulation of water-polymer interactions at the molecular level. By learning from nature and employing sophisticated material engineering, it is possible to create hydrogels that maintain their functionality in some of the most challenging environments on Earth and beyond. The exceptional water content within hydrogels, which can constitute over 95% of their weight, is not a homogeneous reservoir. The physical state and behavior of this water are critically determined by its interactions with the polymer network, leading to a classification into distinct categories based on binding energy and mobility, i.e., ​​free water, intermediate water and bound water (Figure 2)​​.

Figure 2. Illustration of the water states in gel materials.

Free water​​. This fraction exists in the larger pores of the hydrogel network and does not interact directly with the polymer chains. Its properties are nearly identical to bulk water, including a freezing point close to 0 °C. Upon cooling, free water readily forms ice crystals, whose growth can disrupt the polymer network, leading to a catastrophic loss of elasticity and conductivity in flexible applications.

​​Intermediate water. This water layer is associated with the polymer chains through weaker hydrogen bonds or van der Waals forces. It has a depressed freezing point, typically between 0 °C and -40 °C, and does not crystallize as easily as free water. The presence and proportion of intermediate water are crucial for imparting freeze resistance, as it remains in a liquid-like state at subzero temperatures, maintaining segmental mobility and ion transport within the gel.

Bound water​​. This water is tightly bound to hydrophilic groups on the polymer chains (e.g., -OH, -COOH, -NH2) via strong hydrogen bonds. Its freezing point is significantly depressed below -40 °C, and it does not crystallize even under extreme cold. This non-freezable water is essential for maintaining the structural integrity of the hydrogel network at ultra-low temperatures.

The dehydration of hydrogels at elevated temperatures follows a reverse hierarchy; free water evaporates first, followed by intermediate water, while bound water is the most difficult to remove. Understanding and manipulating the relative proportions of these water states is the cornerstone of designing wide-temperature tolerant hydrogels. The primary goal of advanced strategies is to ​​minimize the free water content and maximize the fraction of intermediate and bound water​​.

​​2.2 Bio-inspired water retention strategies​​

Nature has evolved sophisticated mechanisms to protect organisms from freezing and desiccation. These biological strategies provide a rich source of inspiration for material scientists, offering blueprints for designing synthetic hydrogels that can withstand extreme environments. ​​ Organisms in polar regions produce anti-freeze proteins (AFPs) and small-molecule cryoprotectants (e.g., glycerol, trehalose). AFPs adsorb to the surface of nascent ice crystals, inhibiting their growth through a mechanism known as ​​adsorption-inhibition​​. Small molecules act as ​​hydrogen-bond competitors​​, disrupting the tetrahedral hydrogen-bonding network of water and effectively depressing its freezing point. This principle is directly translated into material design by incorporating molecules like glycerol, dimethyl sulfoxide (DMSO), or specific ions (e.g., Li+, Na+) into hydrogels. Cell membranes, with their fluid mosaic structure comprising lipids and proteins, create a semi-permeable barrier that regulates water and solute transport. This concept has been ingeniously adapted to create dynamic, self-healing barrier layers on hydrogel surfaces. For instance, an ​​adaptive lipid-integrated bilayer coating can be constructed on a hydrogel. This coating acts as a barrier to water evaporation, and lipids stored within the hydrogel can migrate to repair cracks formed under mechanical strain, ensuring dynamic water retention.

In many natural systems, water is confined within nanoscale compartments, such as in the capillaries of plant tissues or between protein fibers. This ​​nanoconfinement effect​​ dramatically alters water’s phase behavior, suppressing ice formation. In synthetic hydrogels, this is replicated by creating dense, nano-porous networks or by incorporating nanoparticles that create confined spaces where water molecules are strongly associated with large surface areas. The translation of these natural strategies into material design language involves: (i) ​​Introducing hydrogen-bond competitors​​, for instance, adding small molecules or ions that form stronger associations with water than water-water bonds. (ii) ​​Constructing nano-confined structures. Engineering polymer networks with controlled pore sizes at the nanoscale to limit ice crystal nucleation and growth. (iii) ​​Mimicking amphiphilic structures​​. Creating hydrophilic-hydrophobic heterostructures within the hydrogel to regulate water mobility and create barrier layers, much like cell membranes.

​​2.3 Engineered strategies for extreme temperature tolerance​​

Building on the understanding of water states and bio-inspiration, several key engineering strategies have been developed to achieve unprecedented temperature tolerance in hydrogels, spanning from cryogenic conditions to high temperatures exceeding 100 °C.​​

Water state regulation via additives. This is the most direct approach. By introducing high concentrations of ions or polyhydric alcohols, the average number of hydrogen bonds per water molecule is reduced. This not only depresses the freezing point via colligative effects but also increases the proportion of non-freezable water. A break through “hydro-locking”​​ strategy demonstrates that molecules like sulfuric acid can form hydrate bridges between water molecules and the polymer network, effectively “nailing” water in place and preventing both freezing and evaporation across an extremely wide temperature range.

Figure 3. The anti-freezing/water-locking strategy through regulation of water states.

Solvent system engineering​​. Instead of fighting the phase change of water, a radical strategy is to replace water entirely or partially with organic solvents or DES that have inherently low freezing points and low vapor pressures. These ​​non-aqueous gel systems​​ bypass the problem of ice formation altogether. Common choices include ethylene glycol, glycerol, or ionic liquids, which can themselves form extensive hydrogen-bonding networks with the polymer chains.

Dynamic crosslinking network design. The mechanical resilience of a hydrogel under thermal stress is governed by its crosslink density and the nature of the crosslinks. Incorporating dynamic, reversible bonds, such as hydrogen bonds, metal-coordination bonds, or ionic crosslinks, creates a network that can efficiently dissipate energy. When subjected to stress (e.g., ice crystal formation or thermal expansion), these bonds can break and re-form, preventing catastrophic crack propagation and maintaining structural integrity across a wide temperature range. This design also contributes to valuable properties like self-healing. The following Section 3 will delve into how these universal principles are specifically applied to cellulose-based systems, leveraging its unique chemistry for superior performance.

2.4. Interplay between temperature tolerance and other key gel properties​​

The pursuit of temperature-tolerant gels is fundamentally an exercise in ​​multi-objective optimization​​ of the gel’s nano- and micro-structure. Achieving extreme temperature tolerance in hydrogels is not an isolated goal; it profoundly influences and is influenced by other essential properties such as electrical conductivity, mechanical robustness, adhesion, and self-healing capabilities. The strategies employed to suppress freezing and evaporation often involve fundamental modifications to the gel’s chemical and physical structure, creating synergistic or sometimes competing effects that define the overall material performance.

​​2.4.1. Conductivity under thermal stress​​

The electrical conductivity of hydrogels, whether ionic or electronic, is highly susceptible to temperature-induced phase changes of water. In ionic conductors, conductivity (σ) typically follows an Arrhenius-type temperature dependence, σ ∼ exp(-Eₐ/kT), where Eₐ is the activation energy for ion migration. ​​Freezing​​ immobilizes water molecules, drastically reducing ion mobility and causing a precipitous drop in conductivity. Strategies like introducing high-concentration salts or organic solvents address this dualistically: they depress the freezing point and provide a high concentration of charge carriers (ions), ensuring respectable conductivity even at sub-zero temperatures. Conversely, at ​​elevated temperatures​​, the risk is dehydration, which collapses the ion-transport pathways. The same “water-locking” mechanisms that prevent drying, such as the formation of hydrate bridges with sulfuric acid, are crucial for preserving continuous hydration layers necessary for ion conduction over a wide temperature range. Figure 4 summaries the effects of temperature on the conductivity of gels.

Figure 4. Schematic illustration of the effects of temperature on the conductivity of gels.

​​2.4.2. Mechanical performance across a wide temperature

The mechanical integrity encompassing stretchability, compressibility, and toughness of hydrogels is intrinsically linked to the state of water and the dynamics of the polymer network. At low temperatures, the formation of ice crystals can puncture the polymer network, leading to embrittlement. Effective anti-freezing strategies directly mitigate this damage. More profoundly, additives like salts and polyols act as ​​plasticizers​​ at room temperature, enhancing chain mobility and often increasing stretchability. However, this can sometimes come at the cost of reduced initial modulus or strength. The revolutionary ​​hydro-locking​​ strategy demonstrates a remarkable synergy by anchoring water molecules firmly within the network. It prevents both ice formation and network collapse, enabling the gel to maintain high fracture toughness and an elongation rate of over 4 times even at extreme temperatures from -100 °C to 140 °C. This stability arises because the immobilized water molecules contribute to the energy dissipation mechanisms within the cross-linked network without undergoing deleterious phase transitions.

​​2.4.3. Adhesion and self-healing capabilities​​

The dynamic non-covalent interactions (hydrogen bonds, ionic coordination, hydrophobic associations) that confer temperature tolerance are often the very same mechanisms that enable strong interfacial adhesion and self-healing. A gel capable of forming abundant hydrogen bonds with water to resist freezing will also can form similar bonds with biological tissues or other substrates, enabling robust adhesion even in cold environments. Similarly, ​​self-healing​​ relies on the reversible dissociation and reformation of dynamic bonds within the network. While these bond-exchange processes can be slowed at low temperatures, a well-designed gel with a high density of dynamic bonds ensures that self-healing remains effective over a broad temperature range. For example, zwitterionic poly(ionic liquid) hydrogels and nanocomposite organohydrogels have demonstrated excellent self-healing and stable adhesion at temperatures as low as -20 °C to -40 °C. This underscores a fundamental design principle, i.e., ​​engineering a dynamically cross-linked network with tailored interactions is the key to achieving multi-functionality under thermal stress.​

The most successful designs are those that leverage molecular interactions, such as ion hydration, hydrogen bonding, and dynamic cross-linking, to create synergistic effects, ensuring that the enhancement of one property (e.g., freeze resistance) does not compromise others (e.g., conductivity or self-healing), but rather reinforces the overall robustness and reliability of the gel in practical applications.

​​3. Design, fabrication, and temperature-tolerant strategies of cellulose-based gels​​

​​3.1. Cellulose as a structural platform and its dissolution systems​​

Cellulose, Earth’s most abundant biopolymer, consists of linear chains of β(1→4)-linked D-glucose units. Each anhydrous glucose unit bears three hydroxyl groups, enabling the formation of extensive intra- and intermolecular hydrogen bonds that confer remarkable structural stability and axial stiffness. However, this dense hydrogen-bond network also renders cellulose insoluble in water and most common organic solvents, necessitating specialized solvent systems to disrupt its crystalline structure for gel formation. Based on their origin and structural features, cellulose materials can be classified into several categories. ​​Natural cellulose​​ derives directly from plant sources such as cotton (near-pure cellulose), wood fibers (combined with hemicellulose and lignin), grass fibers (e.g., wheat straw, with shorter fibers and higher non-fiber cell ratios), and bast fibers (e.g., flax and hemp, known for high strength and flexibility). ​​Bacterial cellulose (BC)​​ is synthesized by microorganisms such as Gluconacetobacter xylinus, forming an ultra-pure, nanofibrous three-dimensional network with high water-holding capacity (≥ 98%) and superior mechanical properties. ​​Nanocellulose​​ includes cellulose nanofibers (CNFs) produced through mechanical defibrillation, and cellulose nanocrystals (CNCs) obtained via acid hydrolysis, which exhibit high crystallinity and specific surface area. Additionally, ​​cellulose derivatives​​ are created through chemical modification, such as carboxymethyl cellulose (CMC) and hydroxyethyl cellulose (HEC), which enhance solubility and processability.

The dissolution of cellulose fundamentally relies on ​​disrupting its native hydrogen-bond network​​ through competitive interactions. Advanced solvent systems achieve this via multiple mechanisms: (i) Alkali/urea aqueous systems. Deeply chilled NaOH/urea/H2O mixtures penetrate cellulose fibrils, forming a cellulose-NaOH-urea inclusion complex that prevents chain reassociation and maintains solubility. (ii) Derivatizing solvents​​. N-Methylmorpholine N-oxide (NMMO) and LiCl/DMAc systems temporarily derivatize cellulose hydroxyl groups, effectively breaking the hydrogen-bond network before regeneration in anti-freezing coagulants. (iii) Metal salt solutions​​. Concentrated solutions of ZnCl2, LiBr, or CaCl2 create strong ion-dipole interactions with cellulose hydroxyls. The hydrated metal ions (e.g., Zn2+, Li+) coordinate with oxygen atoms on glucose rings, while halide ions (Cl-, Br-) disrupt hydrogen bonds, collectively reducing crystallinity. (iv) Ionic liquids (ILs) and glycerol-based systems: Urea-based ILs and glycerol solvents dissolve cellulose by forming stronger hydrogen bonds with hydroxyl groups than those between cellulose chains. Similarly, imidazolium-based ionic liquids interact strongly with cellulose hydroxyls, facilitating dissolution under mild conditions. (v) Deep-eutectic solvents (DESs). Systems like ZnCl2/ethylene glycol (EG) or AlCl3/ZnCl2/H2O efficiently disrupt cellulose crystallinity through strong ion-dipole interactions. For instance, Zn2+ and Al3+ ions coordinate with cellulose hydroxyls, while chloride ions penetrate and break hydrogen bonds, enabling rapid dissolution at room temperature. The choice of dissolution system directly influences the subsequent gel’s properties. Systems incorporating ions or hydrogen-bond competitors can impart ​​intrinsic cryoprotection​​ by introducing components that depress water’s freezing point and inhibit ice crystallization.

3.2 Fabrication methods for cellulose-based gels

The fabrication of cellulose gels employs a variety of crosslinking strategies, which can be broadly categorized into physical crosslinking, chemical crosslinking, and innovative system designs that incorporate functional additives. Physical crosslinking relies on non-covalent interactions such as hydrogen bonding, hydrophobic interactions, and ionic bonds. For instance, hydrogen bonds formed between cellulose hydroxyl groups contribute to network stability, while methyl cellulose (MC) undergoes thermal reversible gelation driven by hydrophobic associations upon heating. Ionic bonds involve interactions between charged polymers and counterions; carboxylmethyl cellulose (CMC) can form physical crosslinks with multivalent metal ions like Ca2+ or Fe3+, leading to ion-responsive hydrogels. These physically crosslinked gels often exhibit self-healing properties and stimuli responsiveness, although their mechanical strength may be limited.

Chemical crosslinking creates permanent, covalent networks, enhancing mechanical stability. Etherification reactions using crosslinkers like epoxy chloropropane (ECH) or ethylene glycol diglycidyl ether (EGDE) form ether bonds between cellulose chains. Free radical polymerization is another common method, where initiators generate radicals on cellulose chains, allowing graft copolymerization with monomers such as acrylic acid (AA) or acrylamide (AM). This process can be facilitated by radiation techniques like electron beam irradiation, which avoids the need for chemical initiators. Chemically crosslinked gels typically demonstrate superior mechanical strength and resistance to degradation compared to their physically crosslinked counterparts

Recent innovative strategies focus on constructing composite or hybrid gel systems to achieve multifunctionality. The pre-stretching and orientation strategy, inspired by the noodle-making process, involves applying mechanical stretching to a nascent gel to align cellulose fibers, followed by introducing metal ions like Ca2+ to form coordination bonds. This method can produce hydrogels with exceptionally high tensile strength (up to 52.79 MPa) and fracture toughness. Another approach utilizes polymerizable deep eutectic solvents (PDES), as demonstrated by systems combining ionic liquids (e.g., BmimCl), acrylamide (AM), and cellulose. The strong hydrogen-bonding interactions within the PDES not only facilitate cellulose dissolution but also impart inherent anti-freezing properties and high ionic conductivity to the resulting gels. Additionally, double network (DN) or interpenetrating network (IPN) structures are employed by combining cellulose with a second polymer network, such as polyacrylamide (PAM). In these systems, the rigid cellulose network dissipates energy through sacrificial bond breakage, while the ductile synthetic polymer network maintains overall integrity, resulting in gels with high toughness and elasticity across a wide temperature range.

3.3. Strategic design for freeze-resistance and dehydration prevention​​ in cellulose-based gels

The ability of cellulose gels to withstand freezing and drying stresses stems from sophisticated strategies that manipulate water states and reinforce the polymer network through multi-scale design. A fundamental approach involves the use of nanocellulose to create dense, nano-confined networks. The high surface area of cellulose nanofibers (CNFs) or cellulose nanocrystals (CNCs) provides abundant binding sites for water molecules, significantly increasing the proportion of non-freezable, bound water. These nanostructures physically impede the nucleation and growth of ice crystals. For instance, CNC-reinforced composites can maintain flexibility at extremely low temperatures (e.g., -80°C) due to restricted water mobility within the nanoscale network.

Introducing specific additives that act as hydrogen-bond competitors is a widely employed and effective tactic. Salts such as LiCl, CaCl2, and ZnCl2 dissociate into ions that strongly hydrate water molecules via electrostatic interactions. This hydration effect disrupts the native hydrogen-bonding network of water, depressing its freezing point through colligative effects. High concentrations of these salts can prevent freezing even at temperatures below -40°C. Polyols, including glycerol and ethylene glycol, integrate into the water structure through their own hydroxyl groups, effectively disrupting the tetrahedral arrangement necessary for ice nucleation. Glycerol-containing gels, for example, retain elasticity at -20°C and exhibit low vapor pressure, which also mitigates dehydration at elevated temperatures

Organic-inorganic coordination introduces dynamic, energy-dissipating mechanisms that enhance toughness under thermal stress. Incorporating multivalent metal ions or inorganic phases like clay creates coordination bonds with functional groups (e.g., carboxyl groups in CMC) on the cellulose chains. These bonds can reversibly break and reform under mechanical stress, dissipating energy and preventing crack propagation. A notable example is a cellulose/Fe3+/Zn2+ system that achieves room-temperature self-healing and maintains functionality from -20 °C to 50 °C. Furthermore, multi-network architectures, such as double networks (DN) or interpenetrating networks (IPN), synergistically combine the properties of cellulose with other polymers. In a typical DN hydrogel, a rigid, densely crosslinked cellulose network acts as a sacrificial bond that fractures under stress to dissipate energy, while an interpenetrating, ductile synthetic polymer network (e.g., PAM) ensures macroscopic integrity and large deformation capability. This design enables the gel to maintain mechanical robustness and ionic conductivity even after thousands of stretching cycles at subzero temperatures.

The rational design of cellulose-based gels for extreme temperature tolerance involves a multi-faceted approach that encompasses the selection of dissolution systems, the choice of crosslinking methods, and the strategic incorporation of functional additives or composite structures. By leveraging nanocellulose reinforcement, hydrogen-bond competing agents, dynamic coordination bonds, and multi-network architectures, it is possible to precisely control the state of water within the gel and the mechanical response of the polymer network, thereby achieving unprecedented performance in cryogenic and arid environments.

4. Emerging applications of cellulose-based wide-temperature-tolerant gels​​

The integration of freeze-resistance and dehydration tolerance into cellulose-based gels has unlocked a diverse spectrum of applications that extend far beyond conventional flexible electronics. By maintaining mechanical integrity, ionic conductivity, and functional stability across an extreme temperature range (typically from -60 °C to over 100 °C), these advanced materials are pioneering new frontiers in soft robotics, biomedical engineering, environmental science, and energy storage systems operating under harsh conditions. The strategic manipulation of water states and polymer-network interactions, as detailed in previous sections, directly translates into practical performance metrics that enable these cutting-edge applications.

4.1. Flexible energy storage devices

The most prominent application of temperature-tolerant cellulose gels lies in the realm of flexible and stretchable electronics, where they serve as durable electrolytes, sensors, and functional substrates. Conventional energy storage devices, such as supercapacitors and batteries, suffer from catastrophic performance degradation at sub-zero temperatures due to frozen electrolytes and increased internal resistance. Cellulose-based gel electrolytes address this limitation effectively. For instance, a ​​cellulose/polyacrylic acid/bentonite (ACBH-Zn)​​ hydrogel electrolyte enabled a assembled supercapacitor to achieve a high energy density of 323.4 Wh kg-1 and maintain stable charge-discharge cycles even at -60 °C. The incorporated Zn2+ ions and the nano-confined water within the dense polymer network prevent ice crystallization, ensuring continuous ion transport pathways. Similarly, ​​deep eutectic solvent (DES)-reinforced cellulose nanofiber gels​​ have been used to construct supercapacitors that operate reliably from -20 °C to 60 °C, demonstrating a high specific capacitance of 144.94 F g-1 and 90% capacitance retention after 5,000 cycles. These devices are critical for powering wearable health monitors, space exploration rovers, and automotive sensors in arctic climates.

4.2. Triboelectric nanogenerators (TENGs) and senors

The ability to convert mechanical energy from body movements into electricity is a cornerstone of autonomous wearable systems. Temperature-tolerant cellulose gels serve as both the flexible substrate and the functional component in TENGs. A notable example is a ​​cellulose/ZnCl2-based hydrogel TENG​​ that generated an open-circuit voltage of 38.2 V and a short-circuit current of 0.17 μA. Remarkably, when stretched to 200%, its electrical output increased to 53.7 V and 0.34 μA, and this performance remained stable over 800 cycles from -20°C to 60°C. This stability is attributed to the gel’s maintained viscoelasticity and ion mobility, which prevent the signal attenuation typically observed in frozen or dried hydrogels. Such TENGs can be attached to joints or integrated into clothing to monitor human motion while powering micro-electronics, making them suitable for athletes training in cold environments or for industrial workers in refrigerated facilities.

4.3. Biomedical and health monitoring interfaces​​

The biocompatibility, tunable mechanical properties, and ability to function under physiological temperature variations make cellulose-based wide-temperature gels highly attractive for biomedical applications. Chronic wound management often requires dressings that maintain a moist environment and actively monitor healing, even under febrile conditions or in cool climates. Cellulose gels incorporating agents like glycerol or silk fibroin exhibit excellent water-retention capabilities, preventing wound bed desiccation at elevated skin temperatures. Furthermore, their inherent transparency allows for visual inspection of the wound without removal. When integrated with conductive components like Ag+ ions or carbon nanotubes, these gels transform into ​​smart wound dressings​​ that can sense pH changes or exudate levels, providing real-time data on the wound status. Their adhesive properties, driven by catechol groups from retained lignin or polydopamine, ensure conformal contact with the skin without causing trauma upon removal.

​​ The swelling/deswelling behavior of cellulose gels in response to temperature can be harnessed for controlled drug release. Gels designed with a lower critical solution temperature (LCST) near body temperature can act as thermal switches. For instance, a ​​methylcellulose-based hydrogel​​ loaded with an antibiotic can remain contracted at room temperature, retaining the drug. Upon application to a warm, infected wound site, the gel swells, releasing the therapeutic agent precisely where and when it is needed. This on-demand release profile enhances treatment efficacy and minimizes side effects.

The fundamental principle of anti-freezing gels, suppressing ice crystal formation, is directly applicable to cryopreservation. While an emerging field, cellulose gels incorporating cryoprotectants like DMSO or glycerol can act as advanced biopreservation media. They provide a protective, hydrated microenvironment for cells, tissues, or bio-inks during freezing and thawing processes, reducing ice-induced damage and improving the viability of preserved biological materials for applications in tissue engineering and regenerative medicine.

4.4. Environmental remediation and agricultural technology​​

The high surface area, swelling capacity, and functionalizability of cellulose gels are leveraged in environmental and agricultural sectors, where materials must endure outdoor temperature fluctuations. In arid and drought-prone regions, cellulose-based superabsorbent hydrogels are used as soil amendments to improve water retention. Temperature-tolerant formulations ensure that these gels remain functional across seasons, from freezing winters to hot summers. They absorb irrigation water or rainfall and slowly release it to plant roots, reducing water consumption and improving crop survival rates. By incorporating fertilizers, these gels can also provide controlled nutrient release, enhancing agricultural sustainability.

The abundant hydroxyl and carboxyl groups on modified cellulose, such as carboxymethyl cellulose, can effectively chelate heavy metal ions and adsorb organic dyes from contaminated water. Gels designed with a robust, cross-linked network maintain their structural integrity and adsorption capacity even in cold industrial effluent, unlike many traditional hydrogels that become brittle and inefficient. Their biodegradability also presents an eco-friendly advantage over synthetic polymer adsorbents. Furthermore, certain cellulose gel compositions have been explored for air purification, capturing particulate matter and gaseous pollutants due to their porous structure and functional surface chemistry.

4.5. Soft robotics and actuators​​

In the field of soft robotics, actuators require materials that are soft, compliant, and capable of undergoing large deformations. Temperature-tolerant cellulose gels are ideal candidates for creating joints and grippers that can operate in non-climate-controlled environments, such as deep-sea exploration or extraterrestrial missions. By incorporating responsive components like poly(N-isopropylacrylamide), cellulose gel-based actuators can exhibit temperature-driven bending or contraction, enabling motion without the need for complex internal machinery. Their resilience to freezing ensures that these bio-inspired robots do not fail when exposed to unexpected cold shocks.

Research has demonstrated that cellulose-based gels with Bouligand-type structures, inspired by natural materials like fish scales and crustacean shells, can exhibit exceptional toughness and damage tolerance. These structures, achieved through the controlled self-assembly of cellulose nanocrystals, allow the material to dissipate energy efficiently under stress. This property is crucial for robotic systems that interact with unpredictable environments. Additionally, the intrinsic self-healing capabilities of certain cellulose gel formulations, facilitated by dynamic hydrogen or coordination bonds, allow robotic components to autonomously repair minor damages, extending their operational lifespan in remote or challenging settings where maintenance is difficult.

5. Conclusions and future perspectives​​

5.1 Summary of key advances​​

Cellulose-based gels with wide-temperature tolerance represent a significant breakthrough in soft material science, effectively overcoming the limitations of conventional hydrogels in extreme environments. The rational molecular design strategies—incorporating anti-freezing agents such as lithium chloride and glycerol, reinforcing with nanocellulose, and constructing dynamic crosslinking networks—have collectively enabled these materials to achieve remarkable mechanical robustness, ionic conductivity, and functional stability across an impressively broad temperature range, typically from -80 °C to over 100 °C. Key innovations include the development of advanced solvent systems like deep eutectic solvents and ionic liquids that disrupt cellulose’s inherent hydrogen-bond network while imparting intrinsic cryoprotection through colligative effects and ion hydration. The design of multi-network architectures, such as double-network or interpenetrating structures, successfully combines energy-dissipating sacrificial bonds with ductile polymer chains, enabling stretchability exceeding 700% even at temperatures as low as -40°C. Furthermore, the functional integration of properties including high conductivity, autonomous self-healing, strong adhesion, and stimulus responsiveness has paved the way for their application in flexible electronics, biomedical devices, and environmental technologies.

5.2 Current challenges and limitations​​

Despite substantial progress, several critical challenges impede the widespread commercialization of these advanced materials. A significant trade-off exists between scalability and performance; many high-performing gels rely on expensive solvents or complex synthesis routes, which hinder large-scale production. The long-term stability under cyclic mechanical or thermal loading presents another hurdle, as network fatigue, ionic depletion, or plasticization can lead to diminished conductivity and mechanical integrity over time. Biocompatibility and environmental impact concerns arise from the use of high salt concentrations or synthetic polymer components, necessitating thorough investigation into their cytotoxicity and degradation pathways. Additionally, achieving seamless integration with heterogeneous systems, such as rigid electronic components, remains difficult due to mismatches in mechanical properties like Young’s modulus and interfacial adhesion stability.

5.3 Future research directions​​

Future research should prioritize predictive design tools such as machine learning and molecular dynamics simulations to accelerate the discovery of optimal solvent compositions, crosslinking densities, and additive ratios. These tools can elucidate structure – property relationships and guide the rational design of dynamic bonds for enhanced energy dissipation. Bio-inspired approaches offer promising avenues; for instance, mimicking the ice-recrystallization inhibition properties of antifreeze proteins found in Arctic organisms could lead to synthetic polymers that effectively suppress ice formation. Incorporating dynamic covalent chemistry, including bonds like boronate esters or disulfides that reversibly break and reform under specific stimuli, will enable the development of gels with reprogrammable characteristics such as shape-memory behavior and on-demand degradation.

Additive manufacturing techniques like 3D and 4D printing should be leveraged to create spatially graded gels with localized functionality, allowing for the fabrication of complex, customized architectures that evolve their structure post-fabrication. Embracing circular economy principles is crucial; this involves synthesizing gels from waste biomass and designing them for easy dissociation and recycling. Developing closed-loop lifecycle management systems, including solvent recovery processes, will enhance the sustainability profile of these materials. Furthermore, scaling up green solvent systems and optimizing continuous flow reactors are essential steps toward economically viable industrial production.

​​The application horizon for cellulose-based wide-temperature gels is vast and expanding. In energy storage, gels with wide electrochemical windows and low-temperature conductivity could enable all-soft, biodegradable batteries for use in Arctic research or space missions. Autonomous self-healing systems that integrate microfluidic networks for the continuous replenishment of depleted ions or monomers could provide lifelong functionality in isolated environments. Within biomedical engineering, these materials are poised to advance on-skin electronics, smart wound dressings that monitor healing status, and implantable devices that operate reliably under physiological temperature variations. Their utility in environmental science includes serving as smart water-holding matrices for agriculture in arid regions and as high-efficiency adsorbents for wastewater treatment across seasonal temperature fluctuations.

5.4 Concluding remarks​​

Cellulose-based wide-temperature-tolerant gels signify a paradigm shift in soft material design, transitioning from single-function hydrogels to multi-functional, environmentally adaptive platforms. The integration of green chemistry principles with advanced nanoengineering has unlocked unprecedented performance metrics, including mechanical resilience across a 200°C temperature range, autonomous self-repair capabilities, and biocompatibility, all of which align with global sustainability goals. As research progresses, overcoming challenges related to scalability, intelligent design, and circularity will be paramount to translating laboratory innovations into real-world technologies. These materials are poised to play a pivotal role in addressing pressing societal challenges, from enabling energy-efficient flexible electronics to fostering adaptive medical implants, thereby ushering in an era of truly sustainable, high-performance soft materials for an increasingly extreme global environment.

References